Required Mineral Compositions & Crystal Systems

The following is a list of mineral formulae or approximate compositions you will learn this quarter.

Orthosilicates: tet. Si:O = 1:4; (SiO4)4-

garnet	(Ca,Mg,Fe,Mn)3Al2Si3O12	cubic

grossular	Ca3Al2Si3O12 	cubic

pyrope	Mg3Al2Si3O12 	cubic

almandine	Fe3Al2Si3O12 	cubic

spessartine	Mn3Al2Si3O123 	cubic

forsterite (magnesian olivine)    	Mg2SiO4	orthorhombic

fayalite (ferrous olivine) 	Fe2SiO4 	orthorhombic

sphene	CaTiSiO5

zircon	ZrSiO4

staurolite	Mg Fe Al hydrous silicate

Disilicates: tet. Si:O = 2:7; (Si2O7)6-

epidote	Ca Fe Al hydrous silicate

lawsonite	Ca Al hydrous silicate

# Ring Silicates: tet. Si:O = 1:3; (Si6O18)12-

Tourmaline	Mg Fe Al Li B hydrous ring silicate

Pyroxenes: single chain silicates, tet. Si:O = 1:3; (Si2O6)4-

orthopyroxene	(Fe,Mg)2Si2O6	orthorhombic

enstatite	Mg2Si2O6 	orthorhombic

ferrosilite	Fe2Si2O6 	orthorhombic

clinopyroxene	Ca(Fe,Mg)Si2O6	monoclinic

diopside	CaMgSi2O6 	monoclinic

wollastonite	Ca2Si2O6 	monoclinic

hedenbergite	CaFeSi2O6 	monoclinic

jadeite	NaAlSi2O6 	monoclinic

Amphiboles : double chain silicates, tet. Si:O = 4:11; (Si8O22)12-

orthoamphibole	(Mg,Fe)7Si8O22(OH)2	orthorhombic

tremolite	Ca2Mg5Si8O22(OH)2	monoclinic

actinolite	Ca2Fe5Si8O22(OH)2 	monoclinic

glaucophane	Na amphibole 	monoclinic

hornblende	Ca2(Mg,Fe,Al)5(Al,Si)8O22(OH)8 	monoclinic

Sheet silicates : Si,Al:O = 2:5; [(Si,Al)4O10] 4-

talc	Mg3Si4O10(OH)2

muscovite	KAl2AlSi3O10(OH)2	monoclinic

biotite	K(Fe,Mg)3AlSi3O10(OH)2	monoclinic

chlorite	(Mg5Al)(Al,Si3)O10(OH)8	monoclinic

serpentine	Mg3Si2O5(OH)4

Framework silicates: Si,Al:O = 1:2; (SiO2)0

quartz, alpha	SiO2	trigonal

quartz, beta	SiO2	hexagonal

kyanite, andalusite, sillimanite	Al2SiO5	triclinic, orthorhombic, orthorhombic

K-feldspar (orthoclase, sanidine, microcline)	KAlSi3O8	monoclinic, monoclinic, triclinic

albite (sodic plagioclase)	NaAlSi3O8	triclinic

anorthite (calcic plagioclase)	CaAl2Si2O8	triclinic

nepheline	Na K Al  framework silicate (feldspathoid)

sodalite	Na Al  framework silicate (feldspathoid)

zeolite minerals	Ca Na Al hydrous silicates

Non-silicates

rutile	TiO2	trigonal

corundum	Al2O3	hexagonal

hematite	Fe2O3

magnetite	Fe3O4	cubic

spinel	MgAl2O4	cubic

pyrite	FeS2	cubic

sphalerite/wurtzite	ZnS

molybdenite	MoS2

chalcopyrite	CuFeS2

bornite	Cu5FeS4

galena	PbS	cubic

cinnabar	HgS

orpiment	As2S3

realgar	AsS

calcite/aragonite	CaCO3 	trigonal

dolomite	CaMg (CO3)2	trigonal

halite	NaCl	cubic

gypsum	CaSO4  2H2O

apatite	Ca5(PO4)3(OH)	hexagonal

fluorite	CaF2	cubic